# Product Information

# DEX - Outside corner

# Article No. SWP-80-29146

# EAN – 4751006566569

# Text boxes

| Description: | Special outside corner made from non-woven and a flexible coating. |
| --- | --- |
| Material composition: | Substrate: Two outer layers of polypropylene non-woven Coating: Thermoplastic elastomer, resistant to ageing |
| Application: | Sealing for construction corners in addition with waterproofing tapes |
| Colour: | yellow |
| Side length: (approx.) | 109 - 118 mm |
| Height: (approx.) | 60mm / 90 mm |
| Total thickness (approx): | 0,75 mm |
| Material weight (approx.): | 15 g / piece |
| Resistance to temperature: min. / max. | - 30°C / + 90°C |
| Physical Properties: (approx.) | DIN | Value |
| Burst pressure: max. | External | > 1,5 bar |
| Resistance to water pressure | DIN EN 1928 (Version B) | > 1,5 bar |
| Chemical Properties: | Resistance after storage over 7 days by room temperature in following chemicals | + = resistant 0 = weakened - = non resistant |
| Hydrochloric acid 3% | Internal | + |
| Sulphuric acid 35% | Internal | + |
| Citric acid 100g/l | Internal | + |
| Lactic acid 5% | Internal | + |
| Potassium hydroxide 3% / 20% | Internal | + / + |
| Sodium hypochlorite 0,3g/l | Internal | + |
| Salt water (20g/l Sea water salt) | Internal | + |
| Certified according to DIN EN ISO 9001: 2008 Made in Europe |

Warranty: 5 years warranty for the guaranteed product qualities

Storage: cool and dry, protect against sunlight, use within 24 months after receipt.

The above technical data represent average values. The technical information and application instructions are based on our experience and present knowledge. However, it is each users own responsibility to make trials with the original substrates in order to verify the suitability of our products for the intended purpose, taking into consideration all application related parameters. Please contact us if you have any further questions.